## Slide 1: Data Reproducibility Nanotechnology Knowledge Infrastructure Data Curation
Nano WG, December 4, 2014
Marty Fritts

## Slide 2: Experimental Methods & ILS
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Laboratory 1 | 24.68 | 24.89 | 24.89 | 24.67 | 25.46 | 25.44 | 25.24 | 24.65 | 24.56 | 24.64
Laboratory 2 | 15.7 | 15.56 | 15.47 | 15.4 | 15 | 27.39 | 23.92 | 22.31 | 22.19 | 21.77
Laboratory 3 | 14.16 | 14.38 | 14.24 | 14.27 | 14.2 | 14 | 13.84 | 13.88 | 14.02 | 13.9
Laboratory 4 | 11.6 | 11.7 | 11.6 | 12.2 | 12.3 | 12.7 | 12.7 | 11.9 | 12.3 | 12.6
Laboratory 5 | 28.23 | 27.49 | 24.33 | 17.47 | 18.6 | 19.68 | 16.28 | 19.95 | 19.22 | 15.27
Laboratory 6 | 13.86 | 13.31 | 14.47 | 14.76 | 14.44 | 13.7 | 13.98 | 14.23 | 13.93 | 14.11
Laboratory 9 | 10.8 | 10.3 | 7.1 | 12.3 | 9.9 | 11.4 | 10.2 | 11.3 | 9.2 | 12.4
Laboratory 11 | 17.7 | 21.7 | 22.3 | 18.3 | 16.1
Laboratory 12 | 14.18 | 13.64 | 13.19 | 13.22 | 13.7 | 14.45 | 13.65 | 13.33 | 13.5 | 13.82
Laboratory 17 | 16.4 | 17.4 | 16.9 | 17.4 | 17.9 | 15.2 | 16.4 | 15.8 | 16.1 | 16.7
Laboratory 18 | 12.6 | 12.4 | 13.3 | 13.9 | 14.2 | 14.6 | 14.7 | 14.6 | 14 | 14.6
Laboratory 20 | 13.65 | 13.54 | 13.63 | 13.74 | 13.47 | 13.65 | 13.79 | 13.89 | 13.94 | 13.79
The full study involved the measurement of three NIST gold standard reference materials as well as two dendrimers by PCS, and included additional measurements by TEM, SEM and AFM for comparison
The ASTM interlaboratory study of nanoparticle size measurements using photon correlation spectroscopy (PCS)
The data shown at left are partial results of that study indexed by laboratory number for the smallest gold nanoparticle (about 13.5nm).

## Slide 3: Splitting the dataset
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Laboratory 1 | 24.68 | 24.89 | 24.89 | 24.67 | 25.46 | 25.44 | 25.24 | 24.65 | 24.56 | 24.64
Laboratory 3 | 14.16 | 14.38 | 14.24 | 14.27 | 14.2 | 14 | 13.84 | 13.88 | 14.02 | 13.9
Laboratory 4 | 11.6 | 11.7 | 11.6 | 12.2 | 12.3 | 12.7 | 12.7 | 11.9 | 12.3 | 12.6
Laboratory 6 | 13.86 | 13.31 | 14.47 | 14.76 | 14.44 | 13.7 | 13.98 | 14.23 | 13.93 | 14.11
Laboratory 12 | 14.18 | 13.64 | 13.19 | 13.22 | 13.7 | 14.45 | 13.65 | 13.33 | 13.5 | 13.82
Laboratory 20 | 13.65 | 13.54 | 13.63 | 13.74 | 13.47 | 13.65 | 13.79 | 13.89 | 13.94 | 13.79
Laboratory 22 | 9.5 | 9.6 | 9.5 | 9.8 | 9.6 | 9.99 | 9.6 | 9.8 | 9.8 | 9.8
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Laboratory 2 | 15.7 | 15.56 | 15.47 | 15.4 | 15 | 27.39 | 23.92 | 22.31 | 22.19 | 21.77
Laboratory 5 | 28.23 | 27.49 | 24.33 | 17.47 | 18.6 | 19.68 | 16.28 | 19.95 | 19.22 | 15.27
Laboratory 9 | 10.8 | 10.3 | 7.1 | 12.3 | 9.9 | 11.4 | 10.2 | 11.3 | 9.2 | 12.4
Laboratory 11 | 17.7 | 21.7 | 22.3 | 18.3 | 16.1
Laboratory 17 | 16.4 | 17.4 | 16.9 | 17.4 | 17.9 | 15.2 | 16.4 | 15.8 | 16.1 | 16.7
Laboratory 18 | 12.6 | 12.4 | 13.3 | 13.9 | 14.2 | 14.6 | 14.7 | 14.6 | 14 | 14.6
Laboratories with standard deviations of less than 0.5 for their replicate measurements. Of the seven labs having the lower variability, four are tightly clustered around the “accepted value” of 13.5 nm for the NIST RM. The three other labs show similarly low variability but lie further away from the accepted value. That is these three labs have good replication but don’t “reproduce” the RM sizes
Six labs (with wider variation among their replicates) exhibit both smoothly varying and fluctuating trends in the replicate data, possibly due to lab practice and/or their familiarity with the method and/or their instrumentation. It is significant that the although the protocol for this study stated that repeatability should be within 5%, these laboratories did not attain that threshold.
Other labs, not shown, had greater variability.

## Slide 4: The need - a broader literature?
The data on the previous slides were from the ASTM ILS study for PCS and are a required part of their standard methods. ASTM is considering establishing a collaborative space for its standard protocols to allow dissemination and discussion of method controls, sample preparation techniques, system sensitivities, etc. Such a literature does not yet exist. However, data from disparate sources could be linked through an infrastructure - such as the NKI - to create and sustain it.
The need encompasses modeling and theory as well as experiment.

## Slide 5: Data Curation
The discussion concerning data curation is required to establish what is needed to aid in achieving better reproducibility. Examples – test cases - are needed to advance the discussion in terms of practical steps to establish a literature that provides the means for achieving better reproducibility –for the science, its applications, and its translation to products. The expanded data literature is crucial to that development.